Data Sheet HPS – Black Injection

Product: 			HPS – Back Injection

Color:				Black

Chemical description:		High Impact Polystyrene

Delivery form:		HPS pellets

Appearence:			Black

Packaging:

Big Bags (height x width x depth) 1600 x 950 x 950

delivered on one-way wooden pallet (width x depth) 1200 x 1200

Weight pallet 1000 - 1050

Material Characteristics

| Test type | DIN testing requiremensts/conditions | Measuring unit | Measured value |
| --- | --- | --- | --- |
| Density (23°C) | ISO 1183 | g/ cm3 | 1,030 – 1,055 |
| Volume flow rate | ISO 1133/ 200°C/ 5 kg | cm3/ 10 min | 5,7 – 8,4 |
| Melt flow rate | ISO 1133/ 200°C/ 5 kg | g/ 10 min | 8 - 10 |
| Temperature glass transition | ISO 11357-2 | °C | 90 - 100 |
| The grain size of the granulate |  | mm | 3-5 |
| Filter screen |  | mm | 0,16 |