Data Sheet PMMA - Natur

Product: 			PMMA natur

Color:				Natur

Chemical description:		PMMA

Delivery form:		PMMA pellets

Appearence:			Natural

Packaging:

Big Bags (height x width x depth) 1600 x 950 x 950

delivered on one-way wooden pallet (width x depth) 1200 x 1200

Weight pallet 1000 - 1050

Material Characteristics

| Test type | DIN testing requiremensts/conditions | Measuring unit | Measured value |
| --- | --- | --- | --- |
| Density (23°C) | ISO 1183 | g/ cm3 | 1,02 – 1,26 |
| Volume flow rate | ISO 1133/ 190°C/ 5 kg | cm3/ 10 min | 5,64 – 7,15 |
| Melt flow rate | ISO 1133/ 190°C/ 5 kg | g/ 10 min | 4,01 – 6,404 |
| Melting point | ISO 11357-2 | °C | 160 - 175 |
| The grain size of the granulate |  | mm | 3-5 |
| Filter screen |  | mm | 0,16 |